|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **Product number** | **Type** | **Solid content** | **Recommended use** | **Product characteristics** |
| **AP122** | **Aliphatic Polyurethane** | **29-31%** | **Printing** | **High elongation (more than 1000%), good tensile strength, low temperature resistance, high gloss, excellent anti-backtack.** |